PRODUCT SPECIFICATION BULLETIN

# CERTIFICATE of COMPLIANCE – MALLEABLE IRON PIPE FITTINGS

This letter is to certify that the Malleable Iron Pipe Fittings sold by Quality Pipe Products, Inc. comply with the following specifications.

    - Materials – ASTM A 197

    - Dimensions – ANSI B 16.3

    - Threads – ANSI B 1.20.1

    - Tensile Strength -  28.4KG/MM2

    - Elongation – 5% Minimum

    - Working Pressure – 10KG/CM2 (150PSI)

If you require further information or have questions, please contact us.  Thank you for choosing Quality Pipe Products as your pipe nipple and fitting source.

Sincerely;

Quality Pipe Products, Inc.